承      认     书

| 客户名称 |  |
| --- | --- |
| 品 牌 |  |
| 产 品 | 3.0V扣式锂-二氧化锰电池 |
| 型 号 | CR2025 |
| 制 作 | 张建新 |
| 审 批 | 画帅 |
| 日 期 | 2018-10-18 |

1. 【范围】

本承认书的各种技术参数仅适用于3V锂锰扣式电池CR2025，该电池由力聚电池（湖北）有限公司生产。

2. 【技术参数】

表一：

| 项 目 |  | 单位 | 数值 | 条 件 |
| --- | --- | --- | --- | --- |
| 公称电压 |  | V | 3.0 | 无负载 |
| 公称容量 |  | mAh | 150 | 正常放电的情况下 |
| 瞬时短路电流 |  | mA | ≥250 | 时间≤0.5秒 |
| 开路电压 |  | V | ≥3.20 | 无负载 |
| 贮存温度 |  | ℃ | 0~35 | 室温 |
| 标准重量 |  | g | 2.4 | 每只电池 |
| 放电时间 | 初始值 | 标准值 | 375h | 在负载7.5KΩ、20~25℃的温度、终止电压为2.0V的情况下持续放电时间 |
|  |  | 最小值 | 360h |  |
|  | 经12个月贮存后的数值 | 标准值 | 356h |  |
|  |  | 最小值 | 340h |  |

表二：

| 保存条件 | 条件 | 特性值 |
| --- | --- | --- |
| 自放电率 | 常温常湿条件下贮存12个月 | 不大于3% |

3. 【产品规格和测试方法】

除非特别说明, 所有的测试都在下列常温条件下进行: 环境温度：20~25℃环境湿度：65±20%。见表三

4. 【使用注意事项】

4.1 正确安装和使用电池,防止短路和装错正负极。

4.2 安装前要检查电池极端和所用器具及其接点，以保证清洁和导电，所用器具不能造成短路。

4.3 新电池不要与使用过的电池混用，不同牌号、等级和品种的电池不要混用，以免增加漏液的可能性。

4.4 电池使用后不得加热，充电或其它的手段反复使用，以免发生爆炸、破损和漏液。

4.5 不得将电池投入火中，也不要拆卸电池，以免发生危险。

4.6 妥善保管微型电池，以防幼儿误吞。

4.7 要注意电池的规定贮存期限。

表三：

| 序号 | 测试项目 | 测试方法 | 标 准 |  |
| --- | --- | --- | --- | --- |
| 1 | 外形尺寸 | 用精确度大于0.02mm的游标卡尺测试时，为防止电池短路，卡尺的一端卡头上应贴上一层绝缘材料 | 直径 | 20.0(-0.20)mm |
|  |  |  | 高度 | 2.5(-0.20)mm |
| 2 | 开路电压 | 万用表的精确度不低于0.25%，内阻大于1MΩ | ≥3.20V |  |
| 3 | 瞬时短路 电 流 | 用万用表测试时，每次时间不超过0.5秒，避免重复测试，若需再次测试时，时间间隔应在半小时以上 | ≥250mA |  |
| 4 | 外 观 | 目测 | 外观平整、光洁、 无锈迹 |  |
| 5 | 放电容量 | 在20~25℃的温度和65±20%的湿度的条件下放置8小时以上，在负载7.5 KΩ，终止电压为2.0V的情况下持续放电时间时所测容量(新电：生产后三个月内) | ≥375h |  |
| 6 | 振摔测试 | 将合格样品放在振动机的振台上，启动振动机，振动频率为10-15次/分钟，持续振动一小时 | 电池性能稳定 |  |
| 7 | 高 温 耐漏液测试 | 在45℃的条件下贮存30天 | 无漏液 |  |
| 8 | 过 放 电 耐漏液测试 | 在电池终止电压达到2.0V后，持续放电5小时 | 无漏液 |  |

5. 【3.0V扣式锂-二氧化锰电池剖面图】 （详见第6页）

6. 【放电图】 （详见第7页）

APPROVAL SHEET

| MESSRS |  |
| --- | --- |
| BRAND |  |
| PRODUCT | 3.0V LITHIUM-MANGANESE BUTTON CELL |
| MODEL | CR2025 |
| PREPARED BY | ZHANG JIAN XIN |
| APPROVED BY | HUA SHUAI |
| DATE | OCT. 18, 2018 |

1. 【SCOPE】

This specification applies to the following 3.0v lithium button cell CR2025 made by Liju battery (hubei) Co.Ltd.

2. 【RATINGS】

TABLE Ⅰ：

| ITEM |  | UNIT | SPECIFICATIONS | CONDITIONS |
| --- | --- | --- | --- | --- |
| Nominal voltage |  | V | 3.0 | Standard discharge |
| Nominal capacity |  | mAh | 150 | Standard discharge |
| Instantaneous short–circuit current |  | mA | ≥250 | Time≤0.5 second |
| Off-load voltage |  | V | ≥3.20 |  |
| Storage temperature |  | ℃ | 0~35 |  |
| Standard weight |  | g | 2.4 | Unit cell |
| Service output | Initial | Standard | 375h | Continuous discharge with load 7.5kΩ, till 2.0v end-voltage at 20~25℃ |
|  |  | Minimum | 360h |  |
|  | After 12 months storage | Standard | 356h |  |
|  |  | Minimum | 340h |  |

TABLE Ⅱ：

| ITEM | CONDITIONS | CHARACTERISTICS |
| --- | --- | --- |
| Self-discharge rate | Stored for 12 months at normal temperature, then continuously discharged with 15kΩ load till 2.0v end-voltage | ≤3% |

3. 【PERFORMANCE AND TEST METHODS】

Unless otherwise stated, all the testing is carried out under the condition: environmental temperature, 20℃~25℃; environmental humidity, 65±20%. Please refer to Table Ⅲ

4. 【SUGGESTIONS AND CAUTIONS】

4.1 Install batteries correctly.

4.2 Ensure the contact points to be clean and conductive.

4.3 Do not mix different types, different brands batteries to serve together.

4.4 Do not heat, recharge the batteries.

4.5 Do not dispose of the batteries in fire.

4.6 Keep away from the small children, if swallowed promptly see doctor.

4.7 Pay attention to the producing date.

TABLE Ⅲ:

| No | ITEM | TEST METHODS | STANDARED |  |
| --- | --- | --- | --- | --- |
| 1 | Dimensions | Using vernier caliper (accuracy≥0.02) while avoiding short-circuit | Diameter | 20.0 (-0.20) mm |
|  |  |  | Height | 2.5(-0.20) mm |
| 2 | Off-load voltage | Using multimeter (accuracy≥0.25%) internal resistance≥1MΩ | ≥3.20v |  |
| 3 | Instantaneous short-circuit current | Time of short-circuit should be less than 0.5 second and avoid repeated test within half an hour | ≥250 mA |  |
| 4 | Appearance | Eyeballing | Bright, clean, no rust, no leakage, And no flaw |  |
| 5 | Capacity | Continuously discharge for 8 hours with load 7.5kΩ, temperature at 20~25℃, humidity at 65±20% till 2.0v end-voltage (for fresh battery only: within 3 months ) | ≥375h |  |
| 6 | Vibration test | Put battery on the platform of the vibrations machine, start the machine and adjust the frequency form 10 times per minute to 15 times per minute. keep it running for an hour | Characteristics keep stability |  |
| 7 | Leakage at high temperature | Stored under temperature (45℃) for 30 days | No leakage allowed |  |
| 8 | Over discharge Test | After 2.0v end-voltage, continuously discharged for 5 hours | No leakage allowed |  |

5. 【BENCH SECTION OF 3.0V LITHIUM MANGANESE DIOXIDE BUTTON CELL】

6. 【DISCHARGE CHARACTERISTICS】